COLDSET BLACK 600 RT OS

TECHNICAL INFORMATION LEAFLET

Black suitable to print newspapers.

Especially formulated for medium speed presses equipped with undershoot duct, that require high viscosity and structured inks with short flow.

Here following some examples of rotary presses where the black can be used:

Solna	:	Distributor

Albert	:	A 210 S

Goss	:	Suburban-Urbanite-Community

Harris	: 	Mercury

Suggested storage temperature: 20 - 25°C

Suggested using temperature: 25 - 30°C

### TECHNICAL DATA SHEET

|  | Unit | Standard value |
| --- | --- | --- |
| Laray Viscosity 23 °C | (dPas) | 95 - 110 |
| Tack Inkometer 1200rpm/90F | (gm) | 7,5 – 8,5 |
| Flow | (cm) | 1 - 3 |

This information has been carefully compiled from experience gained in the laboratory and under commercial conditions. However, the product’s performance and its suitability for the customer’s purpose depend on the particular conditions of use and the material being printed. We recommend that customers satisfy themselves that each product meets their requirements in all respects before commencing a print run. All sales are subject to our standard terms and conditions of sale.

| Code: CCK120200 | C.d.C.: 61130 | Date: 16/12/04 | Revision: 0 | page 1 of 1 |
| --- | --- | --- | --- | --- |